Specification for “LITEFLAM” 60/60 Fire-rated Glass Floor System

University of Cyprus, Business Department

## STRUCTURAL GLASS

1.  Glass construction 	Three layers of heat strengthened glass laminated together using two layers 1.52 mm polyvinyl butyrate, as supplied by Eckelt Glas or equivalent.

2.  Glass thickness 	To be nominally 33mm thick comprising 3 x 10mm heat strengthened

3.  Percentage Frit	Top surface of uppermost sheet to be treated with Eckelt Litefloor anti-slip ceramic frit in standard pattern or equivalent.

4.  Colour of Frit 		To be chosen by architect from standard range available (see websites

www.rogerwilde.com or www.eckelt.at for details).

5.  Design Loading		Glass Floor to be designed to take 4.5 KN/M2 in accordance with Table 7.

of BS 6399 Part 1 1984. Glass supported on the steelwork is designed to deflect no more than L/500 under the specified loading. The minimum

edge support for the glass panels is 20-30mm.

6.  Sealant	Seals between panel and edge to be constructed using two-part polysulphide sealant in standard colour

7.  Bedding strip 		Bedding strip between glass and Roger Wilde Patented supporting steelwork to be 60o shore hardness continuous silicone strip in standard colour. Minimum bedding thickness = 5mm.

Glass Manufacturer:	Bruder Eckelt & Co, Glastechnikgeselschaft m.b.H. ,Resthofstrasse 18

4400 STEYR .  AUSTRIA

## FIRE-RESISTANT GLASS		For 60 minutes Integrity/60 minutes insulation Contraflam EI30 20.76 mm thick should be used.

Glass Manufacturer:	Vetrotech Saint-Gobain UK Ltd., Glenewes House, Gateway Drive, Yeadon, LEEDS. LS19 7XY, ENGLAND.

## “LITEFLAM” FRAME	Suitable for glass panels up to 1500mm x 1500mm or 1000mm x 2000mm. The Liteflam Frame consists of the load transfer steel support system (see patent App. No. 0105991.4) together with blah paper, intumescent paper and intumescent paint (up to 60 minutes).

Supplier/Installers:		Roger Wilde Ltd., Chareau House, 1 Miles Street, Oldham. OL1  3NW

Contact:			tel:	00 44 161 624 6824,    (Cambridge Office 01223 527 018)

fax:	00 44 161 627 3770     (Cambridge Office 01223 872 937)